# Product Data: SportTurf Cushion Supreme

Surface America, Inc. • PO Box 157 • Williamsville, NY 14231
Phone: (800) 999-0555 • Phone: (716) 632-8413 • Fax: (716) 632-8324
info@surfaceamerica.com • www.surfaceamerica.com

Pile Weight:	55 oz/sy (8‐year fade warranty)

Face Yarn Type:	Blended polyethylene and nylon, eight‐ply

Yarn Size:	9,400 denier (5,000 denier for polyethylene and 4,400/8 for nylon)

Pile Height:	7/8” (+/‐ 1/8”)

Color:	Green (Color options available via request)

Construction:	Tufted broadloom

Tufting Gauge:	1/4"

Primary Backing:	Dual polypropylene

Secondary Backing:	Urethane pre-coat with 5 mm foam

Seams:	Adhered or Velcro

Finished Roll Width:	12’

Finished Roll Length:	Up to 120’

Base:	Concrete or asphalt

Adhesive(Indoors):	System can be fully or partially adhered to substrate using STA‐1000 synthetic turf adhesive (or approved equal) or attached at seams using heavy-duty double‐sided tape approved for such surfacing applications

Adhesive (Outdoors):	System must be fully adhered to concrete or asphalt